RG59+FTTH

Description

|  | Material | Diameter (mm) |
| --- | --- | --- |
| Inner Conductor | CCS | 0.81 |
| Dielectric | Foamed PE | 3.68 |
| Al Foil | Bonded APA | 3.88 |
| Overall Braid | Al-Mg |  |
|  | FTTH |  |
| Jacket | PVC | 6.05 |

Characteristics

| Capacitance | 52 pF/m |  | SRL 5~1000MHz | 18dB Min. |
| --- | --- | --- | --- | --- |
| Velocity | 82% |  | Impedance | 75 ± 3 ohms |

Attenuation @ 20℃

| Frequency MHz | Attenuation dB/100m | Attenuation dB/100ft |  | Frequency MHz | Attenuation dB/100m | Attenuation dB/100ft |
| --- | --- | --- | --- | --- | --- | --- |
| 55 | 7.66 | 2.34 |  | 500 | 24.51 | 7.48 |
| 100 | 10.48 | 3.20 |  | 600 | 27.10 | 8.27 |
| 250 | 17.00 | 5.19 |  | 750 | 30.56 | 9.32 |
| 300 | 18.74 | 5.72 |  | 1000 | 35.85 | 10.93 |